**100122 DATA SHEET**

Thickness (nominal) .6 mm / 0.023 inch

Weight .6 kg/m² / 0.12 lbs/ft²

Maximum Width 3200 mm / 126 inch

Minimum Pulley or Knife Edge Diameter 4 mm / 0.16inch

(With the recommended joint)

With the recommended joint & reverse flex, 8 mm / 0.31 inch

Overlap joint or Fasteners

Load for 1% Extension 4 daN/cm / 23 lbs/inch

Standard Tension 0.5%

Continuous Operating Temperature Range -30˚ to +80˚C / -22˚ TO +176˚F

Conveying Surface:

 Material Polyurethane

 Feature Matt

 Color White

Underside:

 Material Polyester

 Feature PU Impregnation

 Color White

 Co-Efficient of Friction 0.15

 (on Steel Slide Bed/Drum)

Belt Construction Features 1 Ply monofilament- cover one side

Recommended Jointing Systems: Alternative Splices:

 Single Finger

Anti-Static Yes

FDA Approved Yes