**100127 DATA SHEET**

Thickness (nominal) 0.6 mm / 0.024 inch

Weight 0.59 kg/m² / 0.12 lbs/ft²

Maximum Width 3000 mm / 118.13 inch

Minimum Pulley or Knife Edge Diameter 4 mm / 0.16 inch

(With the recommended joint)

With the recommended joint & reverse flex, 8 mm / 0.32 inch

Overlap joint or Fasteners

Load for 1% Extension 4 N/mm / 23 lbs/inch

Standard Tension 0.5%

Continuous Operating Temperature Range -30˚ to +80˚C / -22˚ TO +176˚F

Number Of Plies / Lateral Construction 1 / Rigid

Conveying Surface:

Material Polyurethane, approx. 0.008 inch thickness

Feature Matt

Color Blue, 85 Shore "A"

Underside:

Material Impregnated Polyester Fabric

Feature Impregnated monofilament Fabric

Color Blue

Co-Efficient of Friction 0.15

(on Steel Slide Bed/Drum)

Belt Construction Features Matt finish top surface provides optimal release

for many food product transfers. Minimal

thickness construction for optimal cooling

effectiveness and efficiency.

Recommended Jointing Systems: Alternative Splices:

Single Finger

Anti-Static No

FDA Approved Yes