**100721 DATA SHEET**

Thickness (nominal) 0.9 mm / 0.037 inch

Weight 0.88 kg/m² / 0.18 lbs/ft²

Maximum Width 3200 mm / 126 inch

Minimum Pulley or Knife Edge Diameter 6 mm / 0.24 inch

(With the recommended joint)

With the recommended joint & reverse flex, 8 mm / 0.32 inch

Overlap joint or Fasteners

Load for 1% Extension 5 N/cm / 29 lbs/inch

Standard Tension 0.5%

Number of Plies 2

Continuous Operating Temperature Range -20˚ to +100˚C / -4˚ TO + 212˚F

Conveying Surface:

 Material Polyester Fabric

 Feature PU Impregnation

 Color Blue

Intermediate Layer: Polyurethane

Underside:

 Material Polyester Fabric

 Feature PU Impregnation

 Color Blue

 Co-Efficient of Friction 0.15

 (on Steel Slide Bed/Drum)

Belt Construction Features Great flexibility for small pulley diameters

Recommended Jointing Systems: Alternative Splices:

 Single Finger Lace, Mechanical fasteners

Anti-Static Yes

FDA Approved Yes