**110315 DATA SHEET**

Thickness (nominal) 2.0mm / 0.078 inch

Weight 1.9 kg/m² / 0.39 lbs/ft²

Maximum Width 3200 mm / 126 inch

Minimum Pulley or Knife Edge Diameter 10 mm / 0.39 inch

(With the recommended joint)

With the recommended joint & reverse flex, 24 mm / 0.94 inch

Overlap joint or Fasteners

Load for 1% Extension 5 daN/cm / 29 lbs/inch

Standard Tension 0.5%

Continuous Operating Temperature Range -30˚ to +100˚C / -22˚ to +212˚F

Conveying Surface:

 Material Polyester spun fabric

 Feature Bare

 Color White

Underside:

 Material Polyester fabric

 Feature Bare

 Color White

 Co-Efficient of Friction 0.25

 (on Steel Slide Bed/Drum)

Belt Construction Features 2 Ply monofilament with spun rough structure

Recommended Jointing Systems: Alternative Splices:

 Single Finger Lace

 Spiral Lace

Anti-Static Yes

FDA Approved Yes