**120216 DATA SHEET**

Thickness (nominal) 1.4 mm / 0.055 inch

Weight 1.4 kg/m² / 0.29 lbs/ft²

Maximum Width 3100 mm / 122 inch

Minimum Pulley or Knife Edge Diameter 25 mm / 1.00 inch

(With the recommended joint)

With the recommended joint & reverse flex, 35 mm / 1.38 inch

Overlap joint or Fasteners

Load for 1% Extension 7 daN/cm / 40 lbs/inch

Standard Tension 0.5%

Continuous Operating Temperature Range -20˚ to +100˚C / -4˚ to +212˚F

Conveying Surface:

Material Polyurethane with negative pyramid profile

Feature Matt

Color White

Underside:

Material Polyester

Feature PU Impregnation

Color White

Co-Efficient of Friction 0.15

(on Steel Slide Bed/Drum)

Belt Construction Features 2 Ply monofilament

With negative pyramid profile

Recommended Jointing Systems: Alternative Splices:

Single Finger Finger Over Lap

Lace

Spiral Lace

Anti-Static Yes

FDA Approved Yes