**130206 DATA SHEET**

Thickness (nominal) 1.3 / 0.051

Weight 1.5 kg/m² / 0.31 lbs/ft²

Maximum Width 3200 mm / 126 inch

Minimum Pulley or Knife Edge Diameter 12 mm / 0.47 inch

(With the recommended joint)

With the recommended joint & reverse flex, 35 mm / 1.40 inch

Overlap joint or Fasteners

Load for 1% Extension 7 daN/cm / 40 lbs/inch

Standard Tension 0.5%

Continuous Operating Temperature Range -20˚ to +100˚C / -4˚ TO +212˚F

Conveying Surface:

Material Polyurethane

Feature Matt

Color Blue

Underside:

Material Non-Fray Polyester

Feature PU Impregnation

Color Blue

Co-Efficient of Friction 0.15

(on Steel Slide Bed/Drum)

Belt Construction Features 2 Ply Non-Fray monofilament- cover one side

Recommended Jointing Systems: Alternative Splices:

Single Finger Lace

Skive

Anti-Static Yes

FDA Approved Yes