**268255 DATA SHEET**

Thickness (nominal) 2.8 mm / 0.110 inch

Weight 3.05 kg/m² / 0.625 lbs/ft²

Maximum Width 3000 mm / 118.13 inch

Minimum Pulley or Knife Edge Diameter 50 mm / 1.97 inch

(With the recommended joint)

With the recommended joint & reverse flex, 60 mm / 2.36 inch

Overlap joint or Fasteners

Load for 1% Extension 10 N/mm / 57.1 lbs/inch

Standard Tension 0.5%

Continuous Operating Temperature Range -10˚ to +80˚C / +14˚ TO +176˚F

Lateral Construction / Intermediate Layer Rigid / PVC

Number of Plies 2

Conveying Surface:

Material PVC, approx. 0.050 inch thickness

Feature Longitudinal Rib

Color Black, 60 Shore "A"

Underside:

Material Polyester

Feature Low Noise

Color White

Co-Efficient of Friction 0.20

(on Steel Slide Bed/Drum)

Belt Construction Features Quiet running whisper weave bottom & high

grip longitudinal rib top. Product is ISO-340

flame retardant compliant

Recommended Jointing Systems: Alternative Splices:

Finger over Finger Mechanical Fastener

Anti-Static Yes

FDA Approved No

USDA Dairy / USDA Meat & Poultry Approved No / No